Setalux D A 870BA

an acrylic polyol with 4.2% OH (calculated on non-volatiles)

丙烯酸多元醇，羟基含量为4.3%（对不挥发分计）

Technical features技术特性

In combination with aliphatic poly-isocyanates:  high build and gloss, excellent mechanical properties and chemical resistance, practically no yellowing under UV-light, high solids content at application viscosity.

与脂肪族聚异氰酸酯交联: 高丰滿度和光泽，优秀的机械性能和抗化学品性，在紫外线照射下不黄变，应用黏度下具有较高的固体份。

Application应用

1	varnishes, clearcoats and solid colour systems for car repair

(cars, trains and tram units etc.)

用于汽车修补漆光油，清漆和实色漆系统。（汽车，火车和运输机械等）

2	industrial topcoats. 工业面漆。

Solvent composition溶剂组成

butyl acetate醋酸丁酯

Specifications规格

| Property性质 | Value规格 | Units单位 | Method方法 SBM * ISO |
| --- | --- | --- | --- |
| Non-volatiles固体份 | 69 - 71 | % | 001G ** 3251 |
| Acid value (as such)酸值 | 6 - 9 | mg KOH/g | 303A 3682 |
| Viscosity (23°C, 100 s-1 ) 黏度 | 2.8 – 4.2 | Pa.s | 012J 3219 |
| Colour (Lico 200)色泽 | max. 50 | APHA | 008F 6271 |
| -OH Content（as such） 羟基含量 (供应值) | 2.8-3.1 | % | 044B |
| Water content 水分含量 | <=0.1 | % | 039A |
| Appearance外观 | clear, free of extraneous matter 清澈透明，无异物 |  | 017A |

* SBM: Nuplex Resins method of determination (available on request)

** spreading agent, xylene use a paperclip to spread out

Typical properties典型特性

Density (20°C)比重	: 1.03	kg/dm3	DIN 53217

Flash point闪点	: 25	°C	DIN 53213

Setalux D A 870BA

Dilutability稀释性

Aliphatics 脂肪族：	white spirit         石油醚	not dilutable    不可稀释

Aromatics芳香族：	xylene                二甲苯	partly dilutable部分可以

Solvesso 100   100号溶剂油	partly dilutable部分可以

Esters         酯类：	ethyl acetate     乙酸乙酯	dilutable          可稀释

butyl acetate     醋酸丁酯	dilutable          可稀释

Ketones      酮类：	acetone            丙酮	dilutable          可稀释

Alcohols      醇类：	ethanol             乙醇	Partlydilutable 部分可稀释

Butanol            丁醇	dilutable          可稀释

Compatibility相溶性

| Desmodur N 75 | + |  |  | Bayer AG |
| --- | --- | --- | --- | --- |
| Desmodur N 3390 | + |  |  | Bayer AG |
| Desmodur L 75 | + |  |  | Bayer AG |
| Tolonate HDB 75 | + |  |  | Rhodia |
| Tolonate HDT 90 | + |  |  | Rhodia |
| Vestanat T 1890 E | + |  |  | Degussa AG |
| CAB-551-0.01 | - |  |  | Eastman Chemicals |
| CAB-531-1 | - |  |  | Eastman Chemicals |
| UCAR Vinyl Resin VAGH | + |  |  | Union Carbide |
| UCAR Vinyl Resin VROH | + |  |  | Union Carbide |
| Nitrocellulose H24 | + |  |  | Hagedorn |

Suitable mixing proportions (calculated on Non-volatiles) are marked +. Combinations in the proportions marked - are not recommended.

Package and store包装和贮存

200kg per steel drum.  200公斤钢桶包装.

Storage should be under cover, out of direct sunlight and avoiding extreme temperature changes.

Under normal storage conditions (5 – 35°C, away from extremes) sealed, unopened containers of this material would have a shelf life of 12 months from the date of manufacture. If it is stored for longer than 12 months, it is recommended that the product is rechecked for suitability in the intended application.

必须密封储存,避免阳光直接照射和极端的温度变化

在5-35°C密封条件下,从生产日期起保质期为十二个月,如果储存超过12个月后,建议对产品进行重新检测以适合于特定应用.